
[image: image1.jpg]


International Journal of Computer Sciences and EngineeringOpen Access
ResearchPaper
Volume-5, Issue-10E-ISSN: 2347-2693
Evaluation of Durability of Ultra High Performance Fibre Reinforced Concrete (UHPFRC) Through Extreme Temperature

A.P. Shelorkar1*, V.R. Chaudhary2,P.D. Jadhao3
1PhD, Student, Department of civil engineering, Karmaveer Kakasaheb Wagh Institute of Engineering Education &Research, Nashik Savitribai Phule Pune University,Pune, India

2ME, Student, Department of civil engineering, Karmaveer Kakasaheb Wagh Institute of Engineering Education &Research, Nashik Savitribai Phule Pune University,Pune, India
3Professor & Head, Deptartment of civil engineering, Karmaveer Kakasaheb Wagh Institute of Engineering Education &Research, Nashik Savitribai Phule Pune University,Pune, India
E-mail:*shelorkar@gmail.com, vikrant508.vc@gmail.com, jpradip11@rediffmail.com*Corresponding Author:   
Available online at: www.ijcseonline.org 
Received: 00/…./2017, Revised: 00/…./2017, Accepted: 00/…./2017, Published: 00/…./2017
Abstract—In the present era of modern concrete technology Ultra High Performance Fibre Reinforced Concrete (UHPFRC) is new cement based material. An inclusion of fibers shows to increases both mechanical and durability properties of UHPFRC. The aim of this study is to determine durability of UHPFRC containing fly ash and Metakaolin. Durability of UHPFRC after exposed to extreme temperature is evaluated. UHPFRC gives better fire resistance.The specimens were exposed to high temperature, specially 200ºC, 400ºC, and 600ºC for 1 hour. The fire resistance of specimen was classified on the basis of their compressive strength and weight loss. Strength loss was not significant at low temperature; up to 200ºC.Metakaolin shows the better performance as compared with fly ash. SEM analysis was also carried out to study effect of extreme temperature on microstructure of UHPFRC.
Keywords—Compressive strength, Fly ash, Metakaolin, Steel fibres, UHPFRC, SEM

I.  Introduction

UHPFRC is relatively new construction material, which is combination of high performance concrete and fibre reinforcement [1, 2]. Due to low water binder ratio, high binder dosage and relatively high fibre dosage in UHPFRC it has superior mechanical properties [3-7]. Silica fume, lime, fly ash and granulated blast furnace slag used as partial clinker replacement in the production of UHPFRC [8, 9].UHPFRC with hybrid fibre reinforced concrete have better mechanical properties than the concrete with only a single type of fibres [10-16]. Rossi was firstly proposed the application of different types of fibre combined in one concrete [17].

However developing construction industry, concrete expect the compressive strength is also required to high flexural strength , workability and durability, which resulted the development of ultra-high performance concrete (UHPC) and UHPFRC [18,19].
The dense matrix with extremely low permeability allows use of UHPFRC, for example as water proofing layer in bridge deck considering economical & practical reasons, only UHPFRC can be used in field application without heat and pressure curing.

Ultra-high performance fibre reinforced concrete is an expansive because high silica fumes content and other expensive raw materials. In most of countries, they demand that to find an alternative to the silica fume. Our choice was to optimize the use of Metakaolin [20, 21].

Water present in fine pores evaporates under temperature extremities and pressure builds up internally. Spalling occur in concrete when stress can’t be withstood. It is unpredictable if can occur during heating or cooling of UHPFRC [22]. This type of concrete not only reduces amount of concreterequired but also increase serviceability anddurability of the resulting structure.
II. MATERIALS AND METHODS
A. Materials

The cement used in this research is ordinary Portland cement (OPC). Standard consistency of cement is 29.2%. Fly ash and Metakaolin is used as a partial replacement in concrete. To make concrete denser it is necessary to used Metakaolin. P63 grade fly ash is used in this study. Quantity and fineness of fly ash plays animportant role. Higher fineness shows higherworkability and strength with early duration of heating. But more fine ash requires more water and addition of water plays an important role in strength thecomparative study of fly ash/Metakaolin is carried out by keeping many parameters offormulation constant (super plasticizer/binder ratio,Metakaolin or fly ash/binder). Steel fibres, 40mm length and 0.6mm diameter, were employed. Poly-carboxylate based super plasticizerwas used. To achieve good flow ability and minimum water/cement ratio it is essential to used super plasticizer in UHPFRC. Tap water was used for mixing purpose. Specific gravity of fine aggregate is 2.5. Fine sand was used of size 2.36-1.18mm.
B. Mixing Procedure 
Materials were mixed in a concrete mixer in following order: cement, sand, micro silica and Metakaolin or fly ash. These materials were dry mixed until they were homogeneous. Then 80% of total water was added and after 2 min remaining 20% water were mixed with super plasticizer and then added to mixture and mixed. Mixing was continued until no dry materials remained. Finally, steel fibre were added and mixed. Total time of mixing of concrete with fly ash is 12 min and with Metakaolin is 15 min.
C. Flow ability of UHPFRC 
After mixing the concrete was placed in a mould (Hagerman cone) on a dry surface. Then cone was lifted straight upwards to allow a free flow of UHPFRC. Two concrete diameters perpendicular to each other were measured after lifting cone and the mean value of the flow is calculated, as shown in figure 1. Permitted value of the flow for UHPFRC is 280±10mm [23].

[image: image18.png],-f"sJCSE




Figure 1 Flow measurement of UHPFRC
D. Curing conditions

The specimens were removed from moulds after 24 hours of casting and placed in curing tank for 28 days at normal room temperature.
E. Heating and cooling details 

The specimen were heated to elevated temperatures (200, 400 and 600ºC) about 1hour inautomatic electric furnace. The specimen were placed in the furnace starting from normal temperature and heated at a rate of 5ºC/min up to required temperature. After heating, the specimen were allowed to cool in furnace and tested after 24 hours.

F. Mixture details
Comparative study was carried out between fly ash/Metakaolin by keeping many parameters of the mixture constant (super-plasticizer/binder ratio, percentage of fly ash and Metakaolin).

Three reference mixtures with fly ash were cast:

· Fly ash with 2% steel fibres. (FA2)

· Fly ash with 3% steel fibres. (FA3)

· Fly ash with 4% steel fibres. (FA4)

The same mixtures with Metakaolin in place of fly ash were also cast:

· Metakaolin with 2% steel fibres. (MK2)

· Metakaolin with 3% steel fibres. (MK3)

· Metakaolin with 4% steel fibres. (MK4)
III. EXPERIMENTAL INVESTIGATION
A. Mix Proportion
Following table shows the mix proportion of UHPFRC with Fly ash (FA) and Metakaolin (MK).
Table 1. Mix design of UHPFRC

	Materials

	Quantity (kg/m3)

	
	Mix 1
	Mix 2

	Cement
	876
	876

	Sand
	1056
	1056

	Micro silica
	44
	44

	Fly ash 
	220
	-

	Metakaolin
	-
	220

	Watercement ratio
	0.22
	0.27

	High Range Water Reducer
	0.94%
	0.94%

	Steel Fibres
	2%, 3%, 4%


B. Compression test

Compression strength was determined using 100mm cubes, after 28 days. Results of compressive strength tests are presented in table II.

Analysis of these results shows that: 

· Compressive strength of the concrete containing Metakaolinisgenerally equivalent to or slightly lower than those of the concrete with fly ash.

· The presence of the steel fibres increases the compressive strength slightly.

· Compressive strength of concrete exposed to temperature up to 200˚C has minor loss in strength as compared to concrete exposed to temperature 400˚C and 600˚C. Following figure shows thearrangement for compression testing. 
[image: image2.jpg]



Figure 2 Compression test on specimen
IV. RESULTS AND DISSCUSSION
For compression test, at least three specimens for each mix were tested. The results of compressive strength of concrete mixes made with OPC, MK and FA are compared. Compressive strength of controlspecimen which was exposed to extreme temperature is decreases drastically as compared to the concrete which was made with fly ash and Metakaolin.UHPFRC made with 4% of steel fibre shows better strength than concrete made with 2% and 3% of steel fibre in both replacements (fly ash/Metakaolin).
Table 2.   Average compressive strength of UHPFRC cubes.

	Name of sample
	Compressive strength (MPa)

	
	Ambient temperature
	After 200˚C
	After 400˚C
	After 600˚C

	CS
	48.2
	37.2
	26.3
	9.56

	FA2
	94.2
	87
	75.1
	52.5

	FA3
	97.4
	93.5
	88.5
	60.4

	FA4
	113.5
	109
	93.2
	70

	MK2
	93.4
	88
	79
	66

	MK3
	96.1
	91.4
	85.7
	72.5

	MK4
	110.8
	101
	90.2
	73


[image: image3.jpg]



Figure 3 Preparation of sample of UHPFRC for SEM analysis
	
[image: image4.png]3000
2500

_ 2000

C)

2 1500

g

= 1000
500

B Ambient

cs

FA2

W 200°C

FA3

FA4

m400°C  m600°C

MK2 MK3 MK4





Figure4. Reduction in mass of UHPFRC after exposed to extreme temperature
	
[image: image5.png]Compressive strength

= Ambient M After 200°C ® After 400°C  After 600°C
120

(MPa)
ooslo e B
5 &3 88

o

CS FA2 FA3 FA4 MK2 MK3 mk4





Figure 5.Compressive strength variation of UHPFRC at different temperature.

	[image: image6.jpg]zaku X3, 8098 Skm B8 SPPU-JEOL




(a)Ambient temperature
	[image: image7.jpg]



(b)200°C temperature
	[image: image8.jpg]Sum 8888 SPPU-JEOL

888

pect

z8kU




(c)600°C temperature

	Figure 6. SEM micrographs of control specimen

	[image: image9.jpg]ZBkYU X3, 888  Sem BEE8 SPPU-JEOL




(a) Ambient temperature
	[image: image10.jpg]ZBKU  X3,88@  Swum 8088 SPPU-JEOL




(b) 200°C temperature
	[image: image11.jpg]



(c) 600°C temperature

	Figure 7. SEM micrographs of UHPFRC with Fly ash

	[image: image12.jpg]28kU  X3,888  Smm 8688 SPPU-JEOL




(a) Ambient temperature
	[image: image13.jpg]Z8kU  X3,888  Swum BBAE SPPU-JEOL




(b) 200°C temperature
	[image: image14.jpg]28ky 3,808  Smm 8089 SPPU-JEOL




(c) 600°C temperature

	Figure 8.SEM micrographs of UHPFRC with Metkaolin


Microstructure image of the UHPFRC with fly ash and Metakaolin cured at ambient temperature and after that exposed to extreme temperature was obtained by scanning electron microscope.Figure 6, 7, 8 shows microstructure of Normal concrete and UHPFRC, before and after exposed to extreme temperature. In the SEM images of sample of normal concrete, one can observe a very dense structure before exposed to extreme temperature after exposed to extreme temperature voids present in concrete gets bigger, from fig 6 , one can observe that concrete after exposed to extreme temperature particales are separetaed and losses its dense structure. Figure 7 shows microstructure image of UHPFRC with fly ash, pores present in this asample at ambient temperature are less as compared to sample exposed to extreme temperature. Microstructure image of UHPFRC with metakaolin shown in fig 8 one can observe a very dense structure at ambient temperature and less number of pores are present as exposed temperature increases particales get separered and pores get bigger.
V. CONCLUSION
Steel fibres in UHPFRC have significant effect on improving compressive strength. Compressive strength of UHPFRC at 200ºC was not compromised, performed exceptionally well. UHPFRC started losing its strength after exposed to temperature 400ºC. Water required for mixing is less for fly ash as compared to Metakaolin.UHPFRC gives better result after exposed to extreme temperature as compared to normal concrete.At 600˚C the control specimens cannot be with stand. From SEM analysis we can conclude that as exposed temperature of UHPFRC increases voids presents in concrete also increases because of strength of concrete reduces.
References:
	[1]
	Aldahdooh, M.A.A., Muhamad Bunnori, N., &Megat Johari, M.A., “Evaluation of ultra-high performance concrete binder content using the response surface method”, Materials & Design , vol. 52, pp. 957-965, 2013.

	[2]
	Ghafari, F., Costa, H., &Duraes, L., “The Effect of nanosilica addition on Flowability, strength and transport properties of ultra-high performance concrete”, Materials & Design , vol. 59, pp. 1-9,2014.

	[3]
	Tuan, NV., Ye, G., Breugel, K., &Copuroglu, O., “Hydration and microstructure of ultra-performance concrete incorporating rice husk ash”, Cement and Concrete Research, vol. 41, pp. 1104-1111,2011.

	[4]
	Tuan, NV., Ye, G., & Dai, B., “The study of using rice husk ash to produce ultra-high performance concrete” Construction and Building Materials, vol. 25, pp. 2030-2035,2011.

	[5]
	Yang, SL., Millard, SG.,Soutsos, MN., Barnett, SJ., & Le, TT., “Influence of aggregate and curing regime on the mechanical properties of ultra-high performance fibre reinforced concrete (UHPFRC)”, Construction and Building Materials, vol. 23, pp. 2291-2298, 2009.

	[6]
	Toledo, RD., Koenders, EAB.,Formagini, S., & Fairbairn, EMR., “Performance assessment of ultra-high performance fibre reinforced cementitious composites in view of sustainability”, Materials and Design , vol. 36, pp. 880-888, 2012.

	[7]
	Yu, R., &Shui, ZH.,“Influence of agglomeration of a recycled cement additive on the hydration and microstructure development of cement bsed materials”, Construction and Building Materials, vol. 49, pp. 841-851, 2013.

	[8]
	Yu, R., Spiesz, P., &Brouwers H.J.H, “Development of an eco-friendly ultra-high performance concrete (UHPC) with efficient cement and mineral admixtures uses”, Cement and Concrete Composites, vol. 55, pp. 383-394, 2015.

	[9]
	Hassan, AMT., Jones, SW., & Mahmud, GH.,“Experimental test methods to determine the uniaxial tensile and compressive behaviour of Ultra High Performance FIbre Reinforced Concrete (UHPFRC)”, Constructin and Building Materials , vol. 37, pp. 874-882,  2012.

	[10]
	Banthia, N., Majdzadeh, F., Wu, J., &Bindiganavile, V., “Fibre Synergy in Hybrid Fibre Reinforced Concrete in Flexure and Direct Shear”, Cement and concrete Composites, vol. 48, pp. 91-97, 2013.

	[11]
	Ganesan, N., Indira, PV.,&Sabeena, MV., “ Bond stress slip response of bars embedded in hybrid fibre reinforced high performance concrete.” Construction and Building Materials, vol. 50, pp. 108-115, 2014.

	[12]
	Yap. SP., Bu, CH., Alengaram, UJ., Mo, KH., &Jumaat, MZ., “Flexural toughness characteristics of steel polypropylene hybrid fibre reinforced oil palm shell concrete”, Materials and Design, vol. 57, pp. 652–659, 2014.

	[13]
	Banthia, N., & Gupta, R., “Hybrid fiber reinforced concrete (HyFRC): fiber synergy in high strength matrices”, Materials and Structure Details, vol. 37, pp. 707–16, 2004.

	[14]
	Banthia, N., &Nandakumar, N., “Crack growth resistance of hybrid fiber reinforced cement composites”, Cement and Concrete Composites, vol. 25, pp. 3–9, 2003.

	[15]
	Yao, W., Li, J., & Wu, K., “Mechanical properties of hybrid fiber-reinforced concrete at low fiber volume fraction”, Cement and Concrete Research, vol. 33, pp. 27–30, 2003.

	[16]
	Park, SH., Kim, DJ.,Ryu, GS., &Koh, KT., “Tensile behaviour of Ultra-High Performance Hybrid Fibre Reinforced Concrete”, Cement and Concrete Composites, vol. 34, pp. 172–184, 2012.

	[17]
	Rossi, P., Acker, P., &Malier, Y., “Effect of steel fibres at two stages: the material and the structure”, Materials and Structure, vol. 2, pp. 436–439, 1987.

	[18]
	Rossi, P., “Influence of fibre geometry and matrix maturity on the mechanical performance of ultra-high performance cement-based composites”, Cement and Concrete Composites, vol. 37, pp. 246–248, 2013.

	[19]
	El-Dieb, AS., “Mechanical, durability and microstructural characteristics of ultra-high strength self-compacting concrete incorporating steel fibres”, Materials and Design, vol. 30, pp. 4286–4292, 2009.

	[20]
	G. Long, X. Wang, &Y. Xie, “Very high-performance concrete with ultrafine powders”, Cement and Concrete Research , Vol. 32, pp. 601–605, 2002.

	[21]
	Richard,P., &Cheyrezy, M. H., “Composition of reactive powder concretes”, Cement and Concrete Research (1995), vol. 25, pp. 1501–1511.



	[22]
	Akca, A.H., &Zihnioglu, N.O, “High Performance concrete under elevated temperature”, Construction and building materials, vol. 44, pp. 317-328, 2013.

	[23]
	Meng, W., Valipour, M., &Khayat K.H., “Optimization and performance of cost effective utra high performance concrete”, Materials and structures, vol. 50, pp. 1-16, 2017.


Authors Profile

[image: image15.jpg]


[image: image16.jpg]


Mr A PShelorkar pursed bachelor’s degree from from Amravati University in 1996 and Master of structural Engineering from University of Pune  in year 2012. He is currently pursuing Ph.D. from Karmaveer Kakasaheb Wagh Institute of Engineering Education andResearch,Nashik,SavitribaiPhulePune University,Pune and currently working as Assistant Professor in Department of Civil Engineering, Nashik District Maratha Vidya Prasarak Samaja’s Karmaveer Adv. Baburao Ganpatrao Thakare College of Engineering,Nashik, since 2008. He is a life member of ISTEsince 2008.He has published more than 04 research papers in reputed international journals. His main research work focuses on Durability of Ultra high Performance Fiber Reinforced Concrete. He has 10 years of teaching experience and 5 years of Research Experience.
Mr. V R Chaudhary pursed Bachelor of Civil Engineering from Mumbai University, mumbai in 2015. He is currently pursuing Master of Structural Engineering, From Savitribai Phule Pune University, Pune.
[image: image17.jpg]


Dr P D  Jadhao pursed bachelor’s degree from Govt. College of Engineering, Amravati in 1991 and master’s degree from Govt. College of Engineering, Pune in 1996. He completed his doctoral from Sant Gadge Baba Amravati Univesity in 2009.Presently working as Professor  & Head of Civil Engineering Department, Karmaveer Kakasaheb Wagh Institute of Engineering Education and Research,Nashik.His areas of interest are Geotechnical Engineering and published papers in national and international journal.

© 2017, IJCSE All Rights Reserved                 1

_1571750845.xls
Chart1

		CS		CS		CS		CS

		FA2		FA2		FA2		FA2

		FA3		FA3		FA3		FA3

		FA4		FA4		FA4		FA4

		MK2		MK2		MK2		MK2

		MK3		MK3		MK3		MK3

		MK4		MK4		MK4		MK4



Ambient

200⁰C

400⁰C

600⁰C

Mass (g)

2350

2188

2000

1960

2390

2380

2330

2120

2540

2490

2210

2290

2610

2520

2390

2290

2430

2420

2200

2100

2500

2430

2250

2140

2550

2470

2200

2090



Sheet1

				Ambient		200⁰C		400⁰C		600⁰C

		CS		2350		2188		2000		1960

		FA2		2390		2380		2330		2120

		FA3		2540		2490		2210		2290

		FA4		2610		2520		2390		2290

		MK2		2430		2420		2200		2100

		MK3		2500		2430		2250		2140

		MK4		2550		2470		2200		2090






_1571750843.xls
Chart1

		CS		CS		CS		CS

		FA2		FA2		FA2		FA2

		FA3		FA3		FA3		FA3

		FA4		FA4		FA4		FA4

		MK2		MK2		MK2		MK2

		MK3		MK3		MK3		MK3

		mk4		mk4		mk4		mk4



Ambient

After 200˚C

After 400˚C

After 600˚C

Compressive strength (MPa)

48.2

37.2

26.3

9.56

94.2

87

75.1

52.5

97.4

93.5

88.5

60.4

113.5

109

93.2

70

93.4

88

79

66

96.1

91.4

85.7

72.5

110.8

101

90.2

73



Sheet1

				Ambient		After 200˚C		After 400˚C		After 600˚C

		CS		48.2		37.2		26.3		9.56

		FA2		94.2		87		75.1		52.5

		FA3		97.4		93.5		88.5		60.4

		FA4		113.5		109		93.2		70

		MK2		93.4		88		79		66

		MK3		96.1		91.4		85.7		72.5

		mk4		110.8		101		90.2		73

				To resize chart data range, drag lower right corner of range.






